## Slide 1: Corrosion Under an Evans Droplet
COMSOL

## Slide 2: Overview
The century-old Evans droplet experiment demonstrates corrosion that is limited by oxygen transport.
This Evans droplet tutorial model defines the corrosion of an iron surface in contact with a water droplet in a surrounding atmosphere that contains both carbon dioxide and oxygen.
The model accounts for the charge and mass transport of a multitude of species as well as iron dissolution, oxygen reduction, carbonic acid equilibria, and iron hydroxide formation.
The model computes the transient and spatial distributions of the various species within the droplet.
A spatial gradient in the pH is demonstrated and is attributed to the complex interplay between the dissolved iron and the carbonic acid.
N2, O2, CO2
H2O
Fe

## Slide 3: Model Definition
Geometry defined in 2D with axial symmetry: An electrolyte droplet covers the metal surface.
The modeled electrolyte species are:
  H+, OH-, Fe2+, O2, CO2, H2CO3, HCO3–, and CO32-.
Homogeneous reactions in the electrolyte:
  H + + OH-  H2O
  CO2 + H2O  H2CO3
  H2CO3  HCO3- + H +
  HCO3-  CO32- + H +
Fixed concentrations are set for O2 and CO2 at the droplet surface boundary facing the air.
Fe electrode
surface boundary
Symmetry line, r = 0
Droplet surface boundary
Model domain

## Slide 4: Model Definition
There is an oxygen reduction reaction at the metal surface that is more dominant at the edge of the droplet:
  4H+ + 4e- + O2 → 2H2O
Iron is oxidized to balance the reduction reaction:
  Fe(s) → Fe2+ + 2e-
Dissolved iron then forms iron hydroxide due to a precipitation reaction at the electrode surface:
  Fe2+ + 2 OH- → Fe(OH)2(s)
Protons are formed by water autoprotolysis to counterbalance the hydroxide ions consumed:
  H2O → H+ + OH-
CO2 is dissolved at the droplet surface and is consumed inside the droplet in homogeneous reactions. This results in a lower pH at the surface of the droplet and a higher pH inside the droplet.
Edge of the droplet
Symmetry line, r = 0
7.155 mm

## Slide 5: Implementation
The Tertiary Current Distribution, Nernst-Planck interface defines the transport of charged and neutral species.
  The water-based model with an electroneutrality charge balance defines cH and cOH as built-in variables and defines the water autoprotolysis equilibrium automatically.
Iron dissolution and oxygen reduction reactions are set using the Electrode Reaction node.
The Fe(OH)2(s) precipitation reaction is set using the Non-Faradaic Reaction node.
Homogeneous reactions are set using the Equilibrium Reaction nodes.

## Slide 6: Results: Iron Concentration
Concentration of iron ions at 30 s and 300 s. The iron ion concentration is slightly higher toward the edge of the droplet.

## Slide 7: Results: Carbon Dioxide Concentration
Concentration of carbon dioxide at 30 s and 300 s. The CO2 concentration is the lowest at the core of the droplet, since it is consumed in a homogeneous reaction.

## Slide 8: Results: pH
pH at 30 s and 300 s. The iron ion concentration is slightly higher toward the edge of the droplet. The pH is lower toward the edge of the droplet due to CO2 dissolution at the surface and higher toward to the core of the droplet due to homogeneous reactions.

## Slide 9: Results: Current Density and Iron Hydroxide Layer
The anodic current density is higher toward the edge of the droplet, indicating a higher corrosion rate. The Fe(OH)2(s) precipitation thickness is higher toward the center of the droplet.

## Slide 10: References
A. Sainz-Rosales et al., “Classic Evans’s Drop Corrosion Experiment Investigated in Terms of a Tertiary Current and Potential Distribution,” Corrosion and Materials Degradation, vol. 3, no. 2, pp. 270–280, 2022.
A. Kahyarian and S. Nesic, “On the mechanism of carbon dioxide corrosion of mild steel: Experimental investigation and mathematical modeling at elevated pressures and nonideal solutions,” Corrosion Science, vol. 173, no. 108719, pp. 1–27, 2020.